ATTACHMENT D

# 104(SPS) – Coordination of Contract Documents

Add the following to Subsection 104.07 Coordination of Contract Documents:

Special Project Specifications (SPS), plans, Forest Service Supplemental Specifications (FSSS), and Standard Specifications (FP-24) are contract documents. A requirement in one document is binding as though occurring in all the contract documents. The contract documents are intended to be complementary and to describe and provide for a complete contract. In case of discrepancy, calculated and shown dimensions govern over scaled dimensions. The contract documents govern in the following order:

- SPS

- Plans

- FSSS; and

- Standard Specifications (FP-24)

# 703(SPS) – R3-G Forest Service Aggregate

Delete 703.05 and replace with the following:

## 703.05 Surface Course Aggregate

- General. Provide hard, durable particles or fragments of crushed stone, crushed slag, or crushed gravel conforming to the following:

  - Gradation 	Table 703-1

  - Los Angeles abrasion, AASHTO T 96 		35 percent maximum

  - Soundness of aggregate using sodium sulfate 	AASHTO T 104, 5 cycles

    - Coarse aggregate 	12 percent loss maximum

    - Fine aggregate 		      12 percent loss maximum

  - Durability index (coarse), AASHTO T 210	35 minimum

  - Durability index (fine), AASHTO T 210	35 minimum

  - Fractured faces, AASHTO T 335 (one or more)	 75 percent minimum

  - Without organic matter and lumps or balls of clay.

  - Liquid limit, AASHTO R 58 and T 89, Method A	35 maximum

| Table 703-1 Surface Course Gradation R3-G and Plasticity Index Limits |  |
| --- | --- |
| Sieve Size | Percent by Mass Passing Designated Sieve (1,2) (AASHTO T 27 & T 11) |
| 1 inch | 100 |
| 3/4 inch | 97 - 100 |
| 3/8 inch | 68 - 85 |
| No. 4 | 45 - 64 |
| No. 16 | 25 - 42 |
| No. 40 | 16 - 29 |
| No. 200 | 8-18 |
| Plasticity index (PI)* | 4-10 |
| *Imported bentonite can be added to meet the specification. If less than 4 PI then add 2% bentonite. |  |

      - Surface course aggregate shall conform to gradation specified in Table 703-1.

(2) Statistical procedures do not apply.