

[bookmark: _Hlk221263991][bookmark: _Hlk220652489]ATTACHMENT D


[bookmark: _Toc163132619][bookmark: _Hlk197412536]
104(SPS) – Coordination of Contract Documents
[bookmark: _Toc163132311]Add the following to Subsection 104.07 Coordination of Contract Documents: 
Special Project Specifications (SPS), plans, Forest Service Supplemental Specifications (FSSS), and Standard Specifications (FP-24) are contract documents. A requirement in one document is binding as though occurring in all the contract documents. The contract documents are intended to be complementary and to describe and provide for a complete contract. In case of discrepancy, calculated and shown dimensions govern over scaled dimensions. The contract documents govern in the following order:
(a) SPS
(b) Plans
(c) FSSS; and
(d) Standard Specifications (FP-24)

[bookmark: _Toc352763805]703(SPS) – R3-G Forest Service Aggregate
Delete 703.05 and replace with the following:
[bookmark: _Toc352763806]703.05 Surface Course Aggregate
(a) [bookmark: S703_05a]General. Provide hard, durable particles or fragments of crushed stone, crushed slag, or crushed gravel conforming to the following:
(1) Gradation 	Table 703-1
(2) Los Angeles abrasion, AASHTO T 96 		35 percent maximum
(3) Soundness of aggregate using sodium sulfate 	AASHTO T 104, 5 cycles
(a) Coarse aggregate 	12 percent loss maximum
(b) Fine aggregate 		      12 percent loss maximum
(4) Durability index (coarse), AASHTO T 210	35 minimum
(5) Durability index (fine), AASHTO T 210	35 minimum 
(6) Fractured faces, AASHTO T 335 (one or more)	 75 percent minimum
(7) Without organic matter and lumps or balls of clay.
(8) Liquid limit, AASHTO R 58 and T 89, Method A	35 maximum



[bookmark: S703_05c]
	Table 703-1
Surface Course Gradation R3-G 
and Plasticity Index Limits

	Sieve Size
	Percent by Mass Passing
Designated Sieve (1,2)
(AASHTO T 27 & T 11)

	1 inch
	100

	3/4 inch
	97 - 100

	3/8 inch
	68 - 85

	No. 4
	45 - 64

	No. 16
	25 - 42

	No. 40
	16 - 29

	No. 200
	8-18

	Plasticity index (PI)*
	4-10

	*Imported bentonite can be added to meet the specification.  If less than 4 PI then add 2% bentonite. 



(1) Surface course aggregate shall conform to gradation specified in Table 703-1. 
(2) Statistical procedures do not apply. 





